## Slide 1: Teaching Armor to Feel Its Own Damage
VBR RESEARCH CAMP 2026
Bio-inspired, self-sensing 3D-printed armor
Lattices modeled on the deep-sea glass sponge and the mantis shrimp, printed in conductive carbon-black PLA and TPU.
VBR Mechanical Engineering Team · Emmet, Raina, Jayden, Jaycen & Peggy

## Slide 2: Dr. Yang Yang & the Yang Lab
MEET OUR MENTOR
Dr. Yang Yang
Associate Professor of Mechanical Engineering, San Diego State University
BACKGROUND
Ph.D. in Physics & Bioengineering, Wuhan University and UCLA (2015)
Postdoc at the USC Center for Advanced Manufacturing
75+ peer-reviewed papers, including Science Advances and Nature Communications
RECENT AWARDS
NSF CAREER Award (2025)
ASME Rising Star in Mechanical Engineering (2025)
SME Outstanding Young Manufacturing Engineer (2022)
THE LAB · BIOINSPIRED 3D PRINTING
Bioinspired structures
Nacre, lobster-claw and cuttlebone-inspired armor
Robotics & wearables
Star-nose-inspired stretchable skin sensors
Biomedical
3D-printed bone implants, painless microneedles
Environmental
Water-repelling surfaces inspired by Salvinia leaves
Where our project comes from: the lab's nacre-inspired 3D-printed armor that senses its own damage (Yang et al., Science Advances, 2019)

## Slide 3: Meet the Team
THE RESEARCHERS
VBR MECHANICAL ENGINEERING TEAM
Emmet
Raina
Jayden
Jaycen
Peggy
Teaching assistant: Preston
HOW WE WORKED
Everyone designed, printed, tested and wrote
Roles rotated: experiments, data, analysis, slides
Daily check-ins with Dr. Yang and our TA

## Slide 4: What We'll Cover
ROADMAP
01
Research & Ideas
The problem, piezoresistance and nature’s designs
02
Design Process & Methods
CAD, 3D printing and the test rig
03
Testing & Results
Four rounds of crush tests, simulations and the shrimp arches
04
Conclusion & Takeaways
Lessons, real-world uses and what’s next

## Slide 5: Research & Ideas
Why armor needs to feel, and what nature taught us
Photo: Yassine Ait Tahit / Unsplash
01
The problem: hidden damage
How plastic can sense
Nature’s blueprints

## Slide 6: Hidden Damage
THE PROBLEM
Today's armor (Kevlar, Dyneema)
Excellent against bullets, weaker against large impacts
Repeated hits cause internal micro-cracks
Damage is often invisible from the outside
Inspection needs infrared thermography or acoustic emission: large, costly equipment
Self-sensing armor
The armor itself is the sensor
Cracks change its electrical resistance
Can be read with a simple multimeter
3D printed, so it can be customized to the wearer
Can we build armor whose electrical signal reveals how much damage it has absorbed?

## Slide 7: How Can Plastic Feel?
PIEZORESISTANCE
Conductive filament is plastic loaded with carbon-black particles. Touching particles form a network of tiny electrical pathways.
Intact: pathways connected
multimeter
Low resistance
Cracked: pathways broken
multimeter
Resistance RISES ▲
load
carbon-black particle
electric current path
Like a city's road grid: close a few streets (cracks) and traffic (current) must detour. Longer detours mean higher resistance.

## Slide 8: Seeing It Happen
LIVE DEMO
A printed lattice, a multimeter and a hammer
Each strike cracks more of the carbon pathways inside the lattice
The meter reading climbs from about 2.0 to 4.2, roughly doubling
No lab equipment: just the printed part, two clips and a meter
That climbing number is the whole idea: the damage shows up as resistance.

## Slide 9: The Mantis Shrimp
NATURE'S IMPACT EXPERT
Its hammer-shaped club strikes at up to 23 m/s, hard enough to crack snail shells, and survives thousands of blows without shattering.
It inspired our flexible, arched TPU designs.
Photo: Nichika Sakurai / Unsplash

## Slide 10: Borrowing From Nature
NATURE'S BLUEPRINTS
Glass sponge
Mantis shrimp club
Bioinspired
Natural-structure images as reproduced in the paper from the cited literature.
Photo: Claus Giering / Unsplash
Deep-sea glass sponge → rigid lattice with diagonal cross-bracing
Mantis shrimp dactyl club → arched, energy-absorbing “bumps”
Nature

## Slide 11: Two Materials, Two Jobs
CONDUCTIVE FILAMENTS
Both filaments conduct electricity, but they behave very differently under load.
CB-PLA
Rigid · carbon-black polylactic acid
Higher conductivity and stiffness
Cracks show up as resistance changes
Used for the glass sponge lattices
CB-TPU
Flexible · carbon-black thermoplastic polyurethane
Bends and springs back
Absorbs shock and vibration
Used for the mantis shrimp arches
Rigid layers to sense damage, flexible layers to soak up impact.

## Slide 12: Design Process & Methods
From CAD models to conductive prints and a test rig
Photo: ZMorph All-in-One 3D Printers / Unsplash
02
Designing the models
From CAD to printed part
The compression rig

## Slide 13: Designing the Models
ONSHAPE CAD
Global variables let us change strut thickness and cell spacing without redrawing.
3 × 4 grid
Sponge · 1.0 mm
Sponge · 1.5 mm
One bump
Two bumps
Three bumps
Four bumps
Five bumps
Control grid
3 × 4 grid · 44 × 44 × 5 mm · 2.0 mm walls
Glass sponge
Same footprint plus diagonal cross-bracing
Mantis shrimp
1 to 5 swept arches · 25 × 15 × 5 mm

## Slide 14: From CAD to Printed Part
FABRICATION
PRINT SETTINGS
Bambu Lab A1 and H2C, sliced in Bambu Studio
0.4 mm nozzle, 15% gyroid infill
Horizontal vs. vertical orientation tested
TAMING FLEXIBLE TPU
Kept dry and loaded without the PTFE tube
Idler screws loosened 1.5 turns, filament hand-fed
WHAT WENT WRONG
Stringing on small features
0.75 mm lattice was too fine for the nozzle: only the frame printed

## Slide 15: Squeeze and Measure
THE TEST RIG
THE RIG
Hand-cranked stand with a 500 N force gauge
16 mm cylindrical tip presses the sample
Digital scale tracks displacement
Multimeter with alligator clips reads resistance
THE METHOD
Every model tested 3 times, results averaged
FreeCAD finite element analysis to predict stress and failure points
Force and resistance are recorded at the same time as each model is crushed.

## Slide 16: Testing & Results
03
Line thickness and spacing
The final design, ten times
Mantis shrimp arches
Four rounds of crush tests, plus simulations

## Slide 17: Four Rounds of Refinement
GLASS SPONGE LATTICE · CB-PLA
Each round kept the winner from the last and changed one variable.
ROUND 1
Line thickness
Plain grid vs. 1.0 to 2.5 mm diagonal lines
1.0 mm
456.73 N avg
ROUND 1.5
Double-check
Added 0.75, 0.9 and 1.25 mm
1.0 mm
still on top
ROUND 2
Line spacing
Offsets from −1.0 to +1.0 mm
+0.5 mm
493.73 N avg
ROUND 3
Final design
1.0 mm lines + 0.5 mm offset, 10 runs + FEA
425.50 N
average peak
Mantis shrimp arches (CB-TPU): 1 to 5 bumps, same 25 × 15 × 5 mm size. Two bumps won at 131.67 N.

## Slide 18: Round 1: Line Thickness
RESULTS · GLASS SPONGE LATTICE
1.0 mm diagonal lines were both the strongest and the most sensitive.
Chart: Average breaking point (N)
| Grid | 1.0 mm | 1.5 mm | 2.0 mm | 2.5 mm
Average breaking point (N) | 309.3667 | 456.733 | 447.7 | 420.1667 | 343.8667
Chart: Change in resistance (kΩ)
| Grid | 1.0 mm | 1.5 mm | 2.0 mm | 2.5 mm
Change in resistance (kΩ) | 0.1229 | 0.5731 | 0.34766 | 0.369 | 0.07233
1.0 mm: 456.73 N vs. 309.37 N for the plain grid, about 48% stronger
Biggest signal: 0.57 kΩ; thick 2.5 mm lines likely masked the micro-cracks (0.07 kΩ)

## Slide 19: Round 1.5: Is 1.0 mm Really Best?
RESULTS · DOUBLE-CHECK
Thinner and in-between lines were added to make sure we hadn’t missed a better option.
Chart: Average breaking point (N)
| 0.75 mm | 0.9 mm | 1.0 mm | 1.25 mm | 1.5 mm
Average breaking point (N) | 165.7 | 323.6333 | 456.733 | 439.4667 | 447.7
Chart: Change in resistance (kΩ)
| 0.75 mm | 0.9 mm | 1.0 mm | 1.25 mm
Change in resistance (kΩ) | 0.0883 | 0.14966 | 0.5731 | 0.4303
1.0 mm stays on top at 456.73 N, with the largest resistance change (0.57 kΩ)
0.75 mm collapsed at 165.7 N: too fine for a 0.4 mm nozzle, so only the outer frame printed

## Slide 20: Round 2: Line Spacing
RESULTS · SPACING OFFSETS
Strength and sensitivity pull in opposite directions.
Chart: Average breaking point (N)
| −1.0 mm | −0.5 mm | Original | +0.5 mm | +1.0 mm
Average breaking point (N) | 455.1 | 462.2666 | 467.8333 | 493.7333 | 465.4
Chart: Change in resistance (kΩ)
| −1.0 mm | −0.5 mm | Original | +0.5 mm | +1.0 mm
Change in resistance (kΩ) | 0.96293 | 0.30493 | 0.5731 | 0.2131 | 1.0892
+0.5 mm offset: strongest at 493.73 N, but the smallest resistance change (0.21 kΩ)
+1.0 mm offset: biggest signal at 1.09 kΩ, but wider gaps made weak points (465.40 N)

## Slide 21: Round 3: The Final Design
RESULTS · TEN RUNS
1.0 mm lines with a +0.5 mm offset, compressed ten times.
━ 10 individual runs ━ Average
Chart: Time (s)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34
Run 1 | 0 | 0 | 0 | 10 | 30 | 60 | 90 | 130 | 170 | 205 | 240 | 280 | 310 | 360 | 420 | 470 | 490 | 495 | 510 | 490 | 470 | 410 | 350 | 310 | 210 | 160 | 110 | 75 | 50 | 30 | 10 | 0 | 0 | 0 | 0
Run 2 | 0 | 0 | 0 | 0 | 10 | 25 | 50 | 105 | 160 | 220 | 270 | 350 | 425 | 450 | 480 | 520 | 450 | 370 | 300 | 0 | 0 | 0 | 0
Run 3 | 0 | 0 | 0 | 0 | 0 | 15 | 35 | 65 | 110 | 160 | 220 | 290 | 385 | 435 | 475 | 485 | 410 | 350 | 325 | 320 | 300 | 260 | 0 | 0 | 0 | 0 | 0
Run 4 | 0 | 0 | 0 | 0 | 5 | 25 | 60 | 110 | 170 | 225 | 310 | 410 | 440 | 235 | 235 | 225 | 200 | 110 | 55 | 30 | 15 | 0 | 0 | 0
Run 5 | 0 | 0 | 0 | 0 | 0 | 0 | 10 | 30 | 80 | 140 | 200 | 260 | 325 | 410 | 450 | 485 | 475 | 505 | 450 | 0 | 0 | 0 | 0 | 0 | 0
Run 6 | 0 | 0 | 0 | 0 | 5 | 20 | 45 | 95 | 160 | 230 | 320 | 420 | 435 | 485 | 440 | 410 | 445 | 420 | 370 | 0 | 0 | 0 | 0
Run 7 | 0 | 0 | 0 | 0 | 0 | 10 | 35 | 90 | 170 | 225 | 310 | 430 | 455 | 490 | 220 | 220 | 210 | 160 | 90 | 40 | 10 | 0 | 0
Run 8 | 0 | 0 | 0 | 0 | 5 | 20 | 45 | 90 | 150 | 200 | 270 | 380 | 420 | 435 | 455 | 465 | 260 | 230 | 170 | 110 | 65 | 35 | 15 | 0 | 0
Run 9 | 0 | 0 | 0 | 0 | 0 | 10 | 35 | 70 | 135 | 200 | 280 | 380 | 450 | 510 | 470 | 435 | 175 | 180 | 140 | 75 | 35 | 10 | 0 | 0
Run 10 | 0 | 0 | 0 | 0 | 5 | 30 | 70 | 120 | 170 | 220 | 300 | 380 | 435 | 445 | 465 | 430 | 260 | 250 | 245 | 220 | 140 | 90 | 50 | 20 | 0 | 0 | 0
Average | 0 | 0 | 0 | 1 | 6 | 21.5 | 47.5 | 90.5 | 147.5 | 202.5 | 272 | 358 | 408 | 425.5 | 411 | 414.5 | 337.5 | 307 | 265.5 | 128.5 | 103.5 | 80.5 | 41.5 | 47.1429 | 42 | 53.3333 | 36.6667 | 75 | 50 | 30 | 10 | 0 | 0 | 0 | 0
Chart: Displacement (mm)
| 0 | 0.37 | 1.1499999999999999 | 1.94 | 2.71 | 3.53 | 4.18 | 4.71 | 5.31 | 6.06
Run 1 | 0.4892 | 0.5464 | 0.5474 | 0.5481 | 0.5536 | 0.6003 | 0.617 | 0.5596 | 0.5596 | 0.6032
Run 2 | 0.5007 | 0.649 | 0.5769 | 0.5581 | 0.5471 | 0.5724 | 0.7282 | 0.7812 | 0.7262 | 0.8387
Run 3 | 0.8309 | 1.0621 | 1.0984 | 1.0098 | 1.0129 | 1.0114 | 1.0389 | 1.1508 | 1.0917 | 1.1508
Run 4 | 0.8414 | 1.3866 | 1.0905 | 0.9725 | 0.889 | 0.8711 | 0.8793 | 0.9585 | 0.9541 | 0.8856
Run 5 | 0.5169 | 0.5175 | 0.6899 | 0.6261 | 0.605 | 0.6104 | 0.653 | 0.6771 | 0.7609 | 0.7609
Run 6 | 0.5664 | 0.7648 | 0.6244 | 0.5953 | 0.598 | 0.619 | 0.6439 | 0.6569 | 0.6468 | 0.6306
Run 7 | 0.5596 | 0.6343 | 0.6905 | 0.6487 | 0.6521 | 0.6324 | 0.6399 | 0.6792 | 0.7349 | 0.6624
Run 8 | 0.6467 | 0.6513 | 0.6757 | 0.5569 | 0.5506 | 0.5796 | 0.6122 | 0.6014 | 0.5877 | 0.5909
Run 9 | 0.66 | 0.8995 | 1.0673 | 0.7652 | 0.7849 | 0.7602 | 0.8111 | 0.8983 | 0.9778 | 0.9929
Run 10 | 0.5477 | 0.5779 | 0.5716 | 0.5591 | 0.5505 | 0.5623 | 0.5951 | 0.5995 | 0.609 | 0.6521
Average | 0.61595 | 0.76894 | 0.76326 | 0.68398 | 0.67437 | 0.68191 | 0.72186 | 0.75625 | 0.76487 | 0.77681
Average curve peaks at 425.50 N; resistance averages a peak of 0.76 kΩ
Ten runs show how much real prints vary, even with identical settings

## Slide 22: Microscopic Cracks
UNDER THE MICROSCOPE
3 mm
Hairline cracks form where struts meet
Under stress, cracks form, some invisible to the naked eye. Each one breaks part of the carbon network, which is what shifts the resistance.
Magnified ×2.6. The circle marks a crack at a joint.

## Slide 23: Simulating the Load
FINITE ELEMENT ANALYSIS · GLASS SPONGE
500 N static load
FreeCAD simulation of the final design, pressed through a 16 mm head to match the real rig. Before loading (left) and fully loaded (right).
Simulated deformation was compared with what we saw in the physical tests.
16 mm
22 mm
0%
100%

## Slide 24: The Mantis Shrimp Arches
RESULTS · CB-TPU
In flexible TPU, two wide arches beat five narrow ones.
Chart: Time (s)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28
1 bump | 0 | 0 | 0 | 0.33333 | 1.6667 | 2.6667 | 5 | 7.3333 | 9.6667 | 12.3333 | 15.3333 | 19.6667 | 26.6667 | 37.6667 | 52 | 76.6667 | 105 | 116.6667 | 109 | 105 | 80 | 43.3333 | 24.3333 | 14 | 7.6667 | 3.6667 | 1.6667 | 0.33333 | 0
2 bumps | 0 | 0 | 2.9333 | 16.9333 | 18 | 19.0667 | 19.2333 | 22.6667 | 29.3333 | 39 | 60.6667 | 95 | 131.6667 | 116.6667 | 85 | 73.3333 | 76 | 50.6667 | 25.3333 | 14.6667 | 9.3333 | 5.3333 | 3.3333 | 2 | 1.3333 | 0.66667 | 0.33333 | 0 | 0
3 bumps | 0 | 0 | 4.5 | 16.15 | 19.8 | 37.25 | 42.5 | 44 | 42.5 | 44 | 47.5 | 62.5 | 86.5 | 95 | 83.5 | 76.5 | 79 | 45 | 20 | 12.5 | 7.5 | 4 | 1 | 0 | 0 | 0 | 0 | 0 | 0
4 bumps | 0 | 4.8333 | 8.5667 | 19.0667 | 33.5 | 38.3 | 47.6333 | 51.1 | 50.2667 | 53.8 | 61.0333 | 68.3333 | 63.7667 | 61.7333 | 75.4333 | 92.3333 | 62.2333 | 46.1667 | 41.9667 | 22.0667 | 15.2 | 11.7667 | 9.3 | 6.2 | 2.9667 | 0.7 | 0
5 bumps | 0 | 0 | 6.8 | 27.7 | 32.1333 | 26.9667 | 27.6667 | 26 | 29 | 38.6667 | 47.6667 | 59.3333 | 99.3333 | 58.3333 | 30 | 28.3333 | 32.3333 | 25 | 9 | 5 | 3.3333 | 1.6667 | 0.66667 | 0 | 0 | 0 | 0 | 0 | 0
Photo: Heidi Bruce / Unsplash
Two bumps: 131.67 N peak. Wider arches likely spread the load better
Four bumps: 92.33 N. Tight arches buckled locally

## Slide 25: Simulating the Arches
FINITE ELEMENT ANALYSIS · 500 N CONSTANT FORCE
0%
50%
75%
100%
The arches bend instead of snapping
Frames at 0, 50, 75 and 100% of a 500 N load on the two-bump TPU design: the arches flex and flatten as the load grows.

## Slide 26: Final Result: The Two-Bump Arch
MANTIS SHRIMP · CB-TPU
“It was squishy, so it could actually absorb force, but not too squishy that it can actually withstand stuff.”
Chart: Displacement (mm)
| 0 | 1.01 | 3.06 | 3.74 | 4.32 | 5.01 | 5.6499999999999995 | 6.1599999999999993 | 6.78 | 7.42 | 7.9000000000000012 | 8.4600000000000009 | 9.0399999999999991 | 9.59
Force | 0 | 11.4333 | 21.9 | 29.6667 | 36.0667 | 38.6333 | 42.6 | 48.7 | 54.1 | 69.3333 | 89.5667 | 108.8 | 153.2 | 196.6333
Chart: Displacement (mm)
| 0 | 1.01 | 3.06 | 3.74 | 4.32 | 5.01 | 5.6499999999999995 | 6.1599999999999993 | 6.78 | 7.42 | 7.9000000000000012 | 8.4600000000000009 | 9.0399999999999991 | 9.59
Resistance | 0.89933 | 0.8458 | 0.55627 | 0.60663 | 0.53197 | 0.53183 | 0.54147 | 0.54613 | 0.54957 | 0.5496 | 0.58307 | 0.56147 | 0.51267 | 0.46563
Average of 3 trials

## Slide 27: Our Final Prototype
PUTTING IT TOGETHER
We tested our results by building a piece of armor from the data we collected.
Two models:
All PLA, using the finalized glass sponge design
A PLA and TPU mix, using the two-bump arch design
MATERIAL: PLA
GLASS SPONGE
MATERIAL: PLA/TPU MIX
MANTIS SHRIMP

## Slide 28: Conclusion & Takeaways
What we learned and where it could go
Photo: Quilia / Unsplash
04
Lessons learned
Real-life applications
Why this matters

## Slide 29: Lessons Learned
REFLECTION
What got in the way
500 N gauge limit: the strongest models couldn't be broken
Hand-cranked loading, so the rate varied between trials
Testing software deleted several finished datasets
Identical prints gave different resistance readings
What's next
Try other materials: PETG and ABS
Motorized, automated loading for consistent tests
Aim: next-generation body armor, sports safety gear and medical prosthetics

## Slide 30: Real-Life Applications
WHERE IT COULD GO
Sports
Shin guards
Helmets
Elbow and shoulder pads
Military & law enforcement
Armor
Protective vests
Medical
Stronger, durable prosthetics
Monitor movement, detect falls
Transportation
Monitor stress and damage during vehicle operation
Machines
Better protection against outside elements

## Slide 31: Why This Matters
IMPACT
Built-in health check
Armor that reports its own damage, without lab equipment
Light and custom-fit
3D printing makes complex lattices practical and lets armor be shaped to the wearer
Beyond the battlefield
Sports safety gear and medical prosthetics could use the same idea
Nature as engineer
Sponges and shrimp solved strength-per-weight long ago. We can borrow their designs

## Slide 32: Behind the Research
VBR RESEARCH CAMP
A TYPICAL DAY
About an hour of instruction from Dr. Yang
Small teams run experiments with teaching assistants
Roles rotate: experiments, data, analysis, slides
Dr. Yang checks in with every group
Around 4 PM, each team reviews results and slides with him
GUEST SEMINARS
Stanford, UW–Madison and USC researchers on multi-material 3D printing, adaptive materials and ultrasound
SCHEDULE
3 weeks of in-person labs and experiments
6 weeks of paper writing for publication
Notes: [Sources]
Image: AI-generated conceptual research-lab illustration, created for this slide. Does not depict the actual camp, lab or named participants.
[/Sources]

## Slide 33: What We Found
SUMMARY
456.73 N
1.0 mm lines were strongest in Round 1, about 48% stronger than a plain grid
0.57 kΩ
1.0 mm also gave the biggest resistance change in Round 1
493.73 N
A +0.5 mm spacing offset made the strongest lattice of all
131.67 N
Two wide TPU arches carried the most load
3D-printed, bio-inspired lattices in conductive plastic can carry real loads and signal stress through changes in their own resistance.
Strength and sensitivity trade off, so designs must balance both.

## Slide 34: Thank You
VBR MECHANICAL ENGINEERING TEAM
Questions?
Emmet · Raina · Jayden · Jaycen · Peggy
With thanks to Dr. Yang Yang, our TA Preston, and Victory Bell Education & Research
Photo: Victoria Druc / Unsplash